# Ready Black Inks

O2 water base inks are ready to use inks which don’t require any alteration. They are a PVC, phthalate & formaldehyde free aqueous ink system optimised for printing on table and automatic machines. They offer a soft hand-feel, elasticity, smoothness, high opacity, matte ­finish & good productivity (choke free). They offer good printability on all type cotton and poly-cotton fabrics. These inks are recommended for direct screen printing on fabrics.

We offer the following products-

1. WB 8100 RFU Black – Premium grade ready to use black ink
2. WB 8200 RFU Pigment Black – Economy grade ready to use black ink

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 5kg, 25kg

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% fixer for better fastness
	2. Add 5-50% Sparkle Clear
	3. Stir well before use
	4. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: WATER RESISTANT EMULSION like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table