# Water Base Clears

O2 water base clears are transparent bases which are PVC, Phthalate & formaldehyde free. WB clears can create the final desired colour by adding pigment concentrates. They help to increase the print softness. They help increase productivity since they reduce choking. It is suitable for all type cotton and poly-cotton fabrics. Water base clears are suggested for use on direct screen printing on a range of fabrics.

We offer the following products-

1. WB 0200 RFU Classic Clear – Premium Grade
2. WB 0230 RFU Fine Clear – Good quality and soft hand feel
3. WB0121 RFU Dynamik Clear – Good quality and soft hand feel
4. WB0210 RFU Sparkle Clear – Good quality and high stretch
5. WB0180 RFU Absolute Clear – Economy grade

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 4kg, 20kg,

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% - 5% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table