# Discharge Inks

O2 offers water base discharge series which alter original colour of the garment to help achieve the desired finish. They are PVC, phthalate & formaldehyde free inks. They offer a soft hand-feel, smoothness, & good productivity (choke free). These inks are suggested for direct screen printing method on fabrics.

We offer the following products-

1. WB 0410 RFU Eco Discharge Base
2. WB 9410 RFU Eco Discharge White

Suitable Fabrics: Dischargeable dark coloured fabric

Packing Sizes- 1kg,5kg, 25kg

## Application:

* Mesh Count: 43T to 90T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: WATER RESISTANT EMULSION like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table