# Flock Printing Adhesive

O2 water base series offer flock adhesive for direct flock. It is compatible with both flock powder and flock sheets. It offers good adhesion and wash fastness. This product is suggested for direct screen printing method onto fabric.

We offer the following products-

1. WB 0120 RFU Flock Adhesive- Premium grade flock adhesive

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 4kg, 20kg

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
  1. Add 2% fixer for better fastness
  2. Stir well before use
  3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Fusing Temperature/Time: 170°C for 10-15 second
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table