# Foil Printing Adhesive

O2 water base series offer a foil printing adhesive which is compatible with both direct and transfer method. It gives good adhesion and wash fastness. This product is recommended for direct screen printing method onto fabrics.

We offer the following products-

1. WB 0140 RFU Foil Base- Premium grade foil adhesive for Direct Foil
2. WB 0145 RFU Foil Base Eco – Economy grade foil adhesive for Direct Foil
3. WB 0142 RFU Foil Transfer Adhesive – Adhesive for foil heat transfer

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 4kg, 20kg

## Application:

* Mesh Count: 54- 100T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Fusing Temperature/Time: 140°C for 10-15 second
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table