# Water Base Glitter Effect

O2 offer a water base special clear for glitter printing. It gives very good adhesion and wash fastness. It is essential to choose your mesh according to the glitter powder. This product is suggested for direct screen printing method on fabrics.

We offer the following products-

1. WB 0135 RFU Glitter Adhesive

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton etc

Packing Sizes- 1kg, 4kg, 20kg

## Application:

* Mesh Count: 10T to 20T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
  1. Add 2% - 5% fixer for better fastness
  2. Stir well before use
  3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table