# Water Base Pearl Effect

O2 offers water base pearl clears which help to get a pearl effect in printing. By adding pigment concentrates to the WB pearl we can achieve a coloured pearl effect. These inks are suggested for direct screen printing.

We offer the following products-

1. WB 0110 RFU Pearl Shine – Clear for pearl effect

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 4kg, 20kg

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% - 5% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table