# Water Base Poly Series inks

O2 water base offers poly series inks for polyester fabric. It is stretchable, offers good wash-fastness, and a soft hand feel. To prevent colour migrations the Barriers Range also available. These inks are suggested for direct screen printing method.

We offer the following products-

1. WB 9090 RFU Poly White – Good quality for polyester fabric
2. WB 0190 RFU Poly Clear – Clear for colour matching
3. WB 8900 RFU Barrier Grey – Premium grade anti-migration
4. WB 8910 RFU Barrier Base – Economy grade anti-migration

Suitable Fabrics: Polyester blended or 100% polyester

Packing Sizes-1kg, 5kg, 25kg

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
  1. Add 2% fixer for better fastness
  2. Stir well before use
  3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: Water Resistant Emulsions like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table