# Process Colour

O2 offers water base process colours for photo prints by direct screen printing. The series is PVC, Phthalate & formaldehyde free inks. It offers high print quality, very soft hand-feel, smoothness, & good productivity (choke free). Offers good printability on all type cotton and poly-cotton fabrics.

We offer the following products-

1. WB 5610 RFU Process Cyan
2. WB 3610 RFU Process Magenta
3. WB 1610 RFU Process Yellow
4. WB 8610 RFU Process Black

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton to name a few.

Packing Sizes- 1kg, 5kg, 25kg

## Application:

* Mesh Count: 90T to 120T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: Water Resistant Emulsion like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table