# Puff Printing Inks

In O2 water base series Puff Base is a speciality product which helps to achieve a puff effect onto fabric by direct screen printing. Colour matching can done by adding concentrates to get the desired coloured puff effect.

We offer the following products-

1. WB 0130 RFU Puff Base – Water Based Puff Effect base

Suitable Fabrics: Suitable for all types of fabrics such as cotton, polycotton etc

Packing Sizes- 5kg, 25kg

## Application:

* Mesh Count: 43- 62T Mesh
* Squeegee Durometer**:** 60/90/60
* Mixture for opaque colours:
	1. Add 2% fixer for better fastness
	2. Stir well before use
	3. Used screens can be cleaned with pressure water
* Curing Temperature/Time: 160°C for 150 seconds
* Stencil: WATER RESISTANT EMULSION like Zebra-133 TEX, Zebra-708
* Washing: Washing test should be done after 24hours
* Printing Machine: Any automatic machine/ table