# LITHO BACK-UP WHITE

Union’s range of Litho Back-up white plastisol inks are a phthalate- free white ink system formulated to have high opacity, high elongation properties. The range offers a smooth finish as well as a good flow ink (choke free). They are designed to meet the demand of specific substrates or can work across many different substrates. This product is used for screen printing method onto litho printed sheets.

## Products

1. JVP 3603 Litho Back-up White L4 – Economy grade
2. JVP 3604 Litho Back-up White L7 – Premium grade

## Application

1. Mesh Count*:* 24T-54T (as per job requirement)
2. Squeezee: 60/90/60
3. Stencil- VIVID Zebra 809
4. Printing Machine- Table/any printing machine
5. Washing- Washing test should be done after 24hours
6. Curing Instructions: Plastisol inks will not air dry. White plastisols will fully cure and withstand repeated washings when the entire ink deposit reaches (149°C).

## *Caution*

*Always test products for curing, adhesion, cracking, opacity, wash ability and other specific requirements before using in production.*