# PRINTABLE ADHESIVE

Union’s range of Plastisol printable adhesives and Gel are a phthalate- free ink system. It is formulated to have high opacity and bonding of inks with fabric. They are designed for the quality transfer labels. It increases the colour strength & bonding of labels onto the fabrics. It is compatible with hot melt powders.

## Products

1. JVP 4010 Printable Adhesive – Premium Grade
2. JVP 4007 New Printable Adhesive – Economy grade and high demand product
3. JVP 4140 Printable Adhesive Spandex – Specially for high stretch fabric
4. JVP 4070 Plastisol Gum – Basic grade adhesive

## Application

1. Mesh Count*:* 24T-48T (as per job requirement)
2. Squeezee: 60/90/60
3. Stencil- VIVID Zebra 809
4. Printing Machine- Table/any printing machine
5. Washing- Washing test should be done after 24hours
6. Curing Instructions: Plastisol inks will not air dry. Plastisol Adhesives will fully cure and withstand repeated washings when the entire ink deposit reaches (160°C).

## *Caution*

*Always test products for curing, adhesion, cracking, opacity, wash ability and other specific requirements before using in production.*